## Slide 1: Low-Carbon Concrete Solutions: Reducing Environmental Impact in Construction
Robert Rescot, Ph.D., P.E.
Executive Director
Notes: Scouting video playlist: https://www.youtube.com/playlist?list=PLo9XIs4IIoGcYppogYqZ4vdSfomO3nrDT

## Slide 2: Learning Objectives
Understand how cement technology has progressed to create concrete that may looks the same but has been engineered to reduce carbon footprints, even up to being carbon negative.
Learn the about the lifecycle of concrete and how it can be rehabilitated, repaired, and/or recycled to make today’s investment into multi-generational investment
Learn about Environmental Product Declarations (EPDs) for cement and concrete that define the carbon footprint created for construction. Contextualizing this against the life cycle of concrete provides useful data for quantifying a carbon footprint and choosing the best suited low carbon concrete options.
Learn about how construction techniques have changed to optimize the use of concrete and how its use opens the door for other environmentally friendly features such as electric vehicle infrastructure.

## Slide 3: Cement Technology

## Slide 7
Are these all the
same concrete?

## Slide 8
Are these all the
same concrete?
NO!

## Slide 9: What is Concrete?
Cement
Water
Coarse Aggregates
Fine Aggregates
Other Chemicals
Air

## Slide 10: What is Cement
Limestone
Clay
Fly Ash
Chalk
Alumina
Shale
Sand
Iron Ore
Kiln Fired @ 1,500-3,000°F

## Slide 12: Variations
Natural impurities in materials
Grain sizes
Material ratios
Heating temperatures
Other additives

## Slide 13: Heat Sources
Fossil fuels
Landfill generated gas
Other waste heat
Tire buring
Nuclear?

## Slide 14: Aggregates
Naturally harvested (quarrying)
Synthethics
  Captured carbon
  Other waste products
    Coffee grounds

## Slide 15: Reducing Cement Content
Supplementary Cementious Materials (SCMs)
  Fly Ash (i.e. from power plants) (c)
  Silca fume (from silicon production) – (d)
  Blast furnace slag (from steel production)
  Shale
  Marble dust (b)
  Calcinated Clays
  Volcanic ash
Cement is (a)
Notes: https://www.researchgate.net/figure/The-samples-of-a-cement-b-marble-dust-c-fly-ash-and-d-silica-fume_fig1_363858044

## Slide 16: Carbon Capture Reusage
Capture C02 emissions from other sources
Inject emissions into wet concrete
C02 will react with other additives to mineralize
Multiple comercialized additives for this

## Slide 17: Reducing C02
Reduce Cement
Alternative Heat Soures for Making Cement
Injecting Captured CO2
Local Sources

## Slide 18
Concrete Can be
Carbon Negative

## Slide 19: Concrete Lifecycle

## Slide 20: Cradle-to-Grave
Concrete construction can last for generations
Obsolete and damaged concrete can be recycled
  Crshed and re-used for new concrete
  Crushed for erosion control
  Landscaping

## Slide 21
Notes: https://springfieldcr.com/

## Slide 22: Causes of Damage
Physical Damage
  Underdesigned
  Unintentional usages (impacts)
  Trees
Water
  Freeze-Thaw
  Corrorion of steel
Chemical Reactions
  De-icing agents
  Chemical spills
Alkali-Silica Reactivity (ASR)
Improper construction

## Slide 23: Concrete Maintenance
Clean expansion joints
Maintain drains
Keep concrete clean and free of chemicals
Advoid physical damage i.e. dragging or scrapping

## Slide 24: Concrete Repairs
Cut/Grinding out damage
Drill in connecting steel
Replace steel
Place concrete
Skim coat
Saw cut/ drill to stop crack propagation
Diamond grind surface

## Slide 25: Environmental Product Declarations - EPDs

## Slide 26
EPDs:
Quantifying
Environmental
Impact

## Slide 28
Unit of Measure:
Global Warming
Potentials (GWP) KG-CO2
(equivalent)

## Slide 29
This Environmental Product Declaration (EPD) reports the impacts for 1 m3 of ready mixed concrete mix, for use in business to-business (B2B) communication meeting the following specifications:
ASTM C94: Ready-Mixed Concrete
UNSPSC Code 30111505: Ready Mix Concrete
CSA A23.1/A23.2: Concrete Materials and Methods of Concrete Construction
CSI Division 03-30-00: Cast-in-Place Concrete

## Slide 31: EPD Considerations
Raw materials sources
Production methods
Transportation
Construction

## Slide 32: Other Conditions NOT in EPD
Site spcific issues
  Conversion of forested land to industrial faciality
  Engandangered speciales
  Water sources
  Runoff
  Waste Disposal Options
  Power sources
Expected life cycle

## Slide 33
Need to factor EPDs
of alternatives to
expected lifecycle -
NOT up-front impact

## Slide 34
EPDs can be part of
procurement
Process.
If you value it, spec it.

## Slide 35: Specifying Low Carbon
Plan, design and engineer design with goals in mind.
Establish a carbon budget. Contractors need flexibility to meet goal.
Consider incentive bid credits for meeting or exceeding goals.
Standards already in place, many suppliers already on board

## Slide 36: GSA Requirements

## Slide 37: Modern Construction

## Slide 39: Advances in Construction
Blended Cement
Admixtures
Fiber Reinforcement
Recyled Materials
Engineering

## Slide 40: Blended Cements
Optimal mix of cement elements
Combines traditional cement with other materials to reduce cement
  Fly Ash
  Slag
  Silica Fume
  Volcanic Ash
  (More)

## Slide 41: Admixtures
Cheicals to alter properties
  Reduce water
  Decrease set time
  Increase set time
  Increase air content
  Increase workability
Hundreds of products to meet specific needs
Curing compounds

## Slide 42: Fiber Reinforcement
Small fibers blended to enhance strength, reduce cracking
Simmilar to geo-textiles
Omni directional enhancement
Fiber types
  Fiberglass
  Polypropylene / Nylon
  Kevlar
  Steel
  Sisal
  Coconut

## Slide 43
Looking
Forward….

## Slide 45
Electric
Trucks
are a
Game Changer

## Slide 46: Electric Vehilce Factors
No transmission – immediate & direct power to wheels
Increased wheel torque
Increased loads (battery + cargo)
Asphalt pavements can not withstand the increased

## Slide 47: Engineering
Enhanced modeling optomizes materials needs
  Helps reduce material needs
  Can compare multiple options to find optimal design
Product testing technology to optomize mix design
  Field testing with maturity meters
  Lab created strength curves
Options for pre-cast, cast-in-place, and ready mixed concrete

## Slide 48: Questions?
?
Visit our Website www.ilcpa.org
Robert Rescot, Ph.D., P.E.
Executive Director rrescot@ilcpa.org
217-553-4756